Introduction

Problem Statement

Marine propulsion shafts must transmit engine torque to the propeller reliably while enduring cyclic torsion/bending and persistent chloride exposure. In this project, the shaft is 4 m long, operates in seawater at roughly 25 °C, and must transmit 200 kN·m at 100 rpm—about 5.2 × 107 cycles over ten years. Untreated carbon steel in such conditions corrodes at ≈ 0.07 mm·yr⁻¹, making both intrinsic corrosion resistance and protection strategies essential. We will apply Ashby’s materials selection methodology—supported by Ansys Granta EduPack—to translate requirements into indices and rank candidates appropriate for these loads and this environment.

Mechanical Screens

Tortional Strength screen

For solid shaft under torque T, the maximum shear stress is,

τ=TrJ=16Tπd3

Here,

J=πd432     ⇒     τ=16Tπd3

Re-arranging for diameter d:

d≥16Tπτallow1/3

Where τallow is the allowable shear strength

Derived performance indices for ranking

Torsion-limited, minimum mass (solid circular baseline)

For a solid circular shaft under torque T :

τmax= TrJ

Where r=outer radius , J=polar second moment of area

For solid shaft,

J=πr42

So,

τmax= 2Tπr3

To avoid yielding (or fatigue failure in shear),

τmax≤τf

Where τf=allowable shear strength of the material

So,

2Tπr3≤τf      ⇒    r3≥2Tπτf

Thus, the minimum radius required is,

rmin=2Tπτf1/3

The mass is

m = ρV=ρ π r2L

Substituting the minimum radius gives:

mmin= ρπ 2Tπτf132L

Group constants (2T,π,L) as geometry/loading factors, leaving only material terms:

mmin∝ ρτf-2/3

So the performance index (P) for a torsion-limited (Mass index):

P=τf2/3ρ      ⇒       log10(τf)=32log10ρ+ 32log10P

** Ensures the shaft does not shear-fail under the design torque.

Interpretation

The plot on a log10Shear Strength -log10Density chart with slope 3/2 guidelines: materials above the line are better for torsional load capacity (safe torque transmission) while keeping shaft mass low.

Stiffness-limited (deflection/angle of twist)

Constraint - Limit angle of twist:

θ=TLGJ≤θmax

For a solid circular shaft, J=πr42 , Enforce the constraint:

TLGπr42≤θmax   ⇒   r4≥2TLπGθmax    ⇒    rmin=2TLπGθmax1/4

Mass, m=ρV=ρπr2L, Substitute rmin:

mmin=ρπL2TLπGθmax1/4

All load/geometry/limit terms are constants for selection. Hence the material-only dependence is,

mmin∝ρG-1/2

So the performance index (P) for a Stiffness-limited (Angle of twist):

P=G1/2ρ  ⇒       log10(G)=2log10ρ+2log10P

** Ensures the angle of twist stays below allowable limits.

Interpretation

The plot on a log10Shear Modulus-log10Density chart with slope 2 guidelines: materials above the line are better for minimizing shaft twist (torsional stiffness) while remaining lightweight.

Sometimes data for G isn’t available in material databases. The we can use,

G=E2(1+υ)

Where υ is Poisson’s ratio & E is Young’s modulus.

Then,

P=E1/221/2 1+υ1/2 ρ

Constraint - Limit deflection:

Take a simple canonical case (results generalize across standard load cases): simply supported beam with central load F Maximum deflection:

δ=FL348EI≤δmax

For a solid circular section, I=πr44, Enforce the constraint:

FL348Eπr44≤δmax    ⇒    r4≥FL312πEδmax  ⇒    rmin=FL312πEδmax1/4

Mass, m=ρV=ρπr2L, Substitute rmin:

mmin=ρπLFL312πEδmax1/4

All load/geometry/limit terms are constants for selection. Hence the material-only dependence is,

mmin∝ρE-1/2

So the performance index (P) for a Stiffness-limited (Deflection/Alignment):

P=E1/2ρ  ⇒       log10(E)=2log10ρ+2log10P

** Ensures the shaft does not sag beyond bearing alignment tolerance.

Interpretation

The plot on a log10Young’s Modulus-log10(Density) chart with slope 2 guidelines: materials above the line are better for resisting deflection and maintaining alignment while keeping shaft mass low.

Additional Case: Bending Strength-Limited (Yield/Failure)

If instead of deflection, the governing criterion were yielding in bending, the derivation parallels the torsion case:

Maximum bending stress in a circular shaft:

σmax=MyI=MrI

Where M is bending moment, r is outer radius and I=πr44

Constraint: σmax≤ σf (allowable tensile/bending strength),

Rearranging gives a minimum radius,

rmin=4Mπσf1/3

Mass, m=ρV=ρπr2L, Substitute rmin:

mmin=ρπL4Mπσf2/3

All load/geometry/limit terms are constants for selection. Hence the material-only dependence is,

mmin∝ρσf-2/3

So the performance index (P) for a bending strength-limited (yield/Fracture):

P=σf2/3ρ  ⇒       log10(σf)=32log10ρ+32log10P

Interpretation

The plot on a log10Young’s Modulus-log10Density chart with slope 3/2 guidelines materials above the line are better for resisting bending yield/failure at minimum mass. For long, slender shafts this case rarely governs, but it is included for completeness of this analysis.

Discussion: Why This Case Rarely Governs for Marine Shafts

- For a long slender shaft (L = 4 m), deflection under its own weight and under propeller thrust dominates well before bending stress reaches yield.

- Classification rules (ABS, DNV, Lloyd’s) generally require stiffness checks (alignment/deflection) to be satisfied first, because once stiffness is adequate, bending stresses are usually far below yield.

- Therefore, in practice, E1/2ρ is the governing index for shaft alignment, while σf2/3ρ is included here for completeness and to demonstrate the methodology.

Cost - weighted variants

Torsion, strength-limited cost index:

If the price of the material is Cm (currency per unit mass), then the material cost of the shaft is:

Cost=mCm

But, 
mmin∝ρτf-2/3

So,

Costmin∝ρτf-2/3Cm

All load/geometry/limit terms are constants for selection. Hence the material-only dependence is,

Costmin∝(Cmρ) τf-2/3

Here (Cmρ) is cost per unit volume.

So, the performance index (P) for a Torsion, strength-limited cost:

P=τf2/3(Cmρ)  ⇒       log10(τf)=32log10Cmρ+32log10P

Interpretation: On a log10Shear strength-log10cost per unit volume chart, slope 3/2 guidelines modified by material price: materials above the line deliver the cheapest safe torque transmission per weight.

Torsional Stiffness-Limited (Twist) Cost Index

From torsional stiffness case,

mmin∝ ρ G-1/2

So,

Cost ∝ CmρG-1/2

Thus, the cost-weighted index is:

P=G1/2Cmρ    ⇒       log10(G)=2log10Cmρ+2log10P

Interpretation: On a log10Shear Modulus-log10cost per unit volume chart, slope 2 guidelines adjusted for cost: materials above the line provide the best torsional rigidity per cost.

Bending Stiffness-Limited (Deflection) Cost Index

From bending stiffness case,

mmin∝ ρ E-1/2

So,

Cost ∝ CmρE-1/2

Thus, the cost-weighted index is:

P=E1/2Cmρ     ⇒       log10(E)=2log10Cmρ+2log10P

Interpretation: On a log10Young's Modulus-log10cost per unit volume chart, slope 2 guidelines adjusted for cost: materials above the line give better alignment control per cost.

Bending Strength-Limited (Yield) Cost Index

From bending strength case,

mmin∝ ρ σf-2/3

So,

Cost ∝ Cmρσf-2/3

Thus, the cost-weighted index is:

P =σf2/3Cmρ     ⇒       log10(σf)=32log10Cmρ+32log10P

Interpretation: On a log10Tensile Strength-log10cost per unit volume  chart, slope 3/2 guidelines adjusted for cost: materials above the line provide the lowest-cost resistance to bending failure. In long slender shafts, stiffness typically governs, but this case is included for completeness.